Technical Specifications

Polyaluminium Chloride Hydroxide Sulfate – Al2O3 content 10% - Al(OH)a  Clb  (SO4)c

Product Category: Inorganic Polymer

Chemical Family:  Polynuclear Inorganic Salt

Product Standard: EN 883 (or similar standard) TYPE1 NSF 60

Product Name: Polyaluminium Chloride Hydroxide Sulfate

Form / Physical condition: Liquid

Appearance: Clorless to light yellow

No odor

| pH (in water) @ 20(°C) | 2,0- 3,0 |
| --- | --- |
| Freezing point/range (°C) | -18 |
| Boiling point/range (°C) | >100 |
| Melting point (°C) | -18 |
| Flash Point (°C)closed cup | None |
| Ignition temperature (°C) | Not self-igniting |
| Specific Gravity gr/cm3 | None |
| Solubility in water g/l @ 20°C | Miscible |
| Partition coefficient n-Octanol/Water (log Po/w) | Not available |
| Al2O3 | 9,0‐10,3 |
| Density (25°C) (g/cm3) | 1,220‐1,260 |
| pH (in %5 solutıon) | 4±0,5 |
| Basicity (%) | 62‐72 |
| Sulphate (SO4) (%) | <5 |

| Explosive Property | None |
| --- | --- |
| Oxidation Property | None |
| Density (g/cm3) | 1,25 ± 0,1 |
| Viscosity (mPa.s) @ 20(°C) | 5 |

AREAS OF USAGE: Drinking water treatment processes

Delivery type: with IBC (PE) containers